## Slide 1: Machine Learning Framework for Impurity Level Prediction in Semiconductors
Arun Mannodi-Kanakkithodi✢, Michael Toriyama✢, Fatih G. Sen✢, Michael J. Davis✵, Maria K.Y. Chan✢ ✢Center for Nanoscale Materials, Argonne National Laboratory
✵Chemical Sciences and Engineering, Argonne National Laboratory
0

## Slide 2: Impurity Levels in Semiconductors
Experimental
Sample preparation difficult with DLTS or CL.
Difficult to assign observed levels to particular defect.
Density Functional Theory (DFT)
Large supercells, charge states  expensive.
Prior knowledge not utilized for new defect levels.
CHALLENGES
1

## Slide 3: Predicting Impurity Behavior in Semiconductors
Semiconductor + impurity
“Computational Study of Pb Substitution in MAPbBr3”, Chem. Mater. (2019).
"Machine-learned impurity level prediction for Cd chalcogenides”, npj Comput. Mater. (2020).
“Impurity Level Prediction and Screening in Halide Perovskites using Machine Learning”, in prep.
Density Functional Theory
Ef(q) = E(Dq) – E(bulk) + ∑niµi + q(EF+Evbm) + Ecorr
Impurity levels: 𝜀(q1/q2) = [ Ef(q1) - Ef(q2) ] / (q2-q1)
-1/-2
+2/+1
Impurity levels 𝜀(q1/q2):
Fermi energies (EF) where defect transitions from one stable charge state (q1) to another (q2)
Descriptors (X)
Elemental properties
Coordination environment
Unit cell defect calculations
Machine Learning
Linear correlation coefficients between X and P
Regression (eg. random forest) model  P = f(X)
Expensive DFT Computation
ML prediction On-demand
2

## Slide 4: DFT Dataset for Machine Learning
3
CdX | Doping Site | M | ∆H(Cd-rich) | ∆H(Mod) | ∆H(Te-rich) | (+3/+2) | (+2/+1) | (+1/0) | (0/-1) | (-1/-2) | (-2/-3)
CdTe | M_Te | N | 2.09 | 2.48 | 2.88 | -0.97 | -0.67 | -0.40 | -0.08 | 1.44 | 1.90
CdTe | M_Te | O | 1.17 | 1.17 | 1.43 | -0.91 | -0.65 | -0.33 | 0.95 | 1.37 | 2.11
CdTe | M_i_Te_site | Rh | 3.46 | 3.93 | 4.88 | -0.52 | 0.05 | 0.56 | 1.12 | 1.83 | 2.14
CdTe | M_Te | Re | 6.75 | 7.22 | 7.70 | 0.68 | -0.49 | -1.05 | 0.61 | 1.72 | 2.18
CdSe | M_Se | Si | 2.59 | 3.27 | 5.21 | -0.64 | -0.33 | 0.30 | 0.70 | 1.10 | 2.21
CdTe | M_Cd | Be | 0.58 | 0.46 | 0.34 | -0.92 | -0.65 | -0.32 | 1.40 | 1.84 | 2.22
CdTe | M_i_Cd_site | F | 1.72 | 1.48 | 1.24 | -0.85 | -0.56 | -0.29 | 0.03 | 1.77 | 2.23
CdTe | M_i_Te_site | F | 2.61 | 2.38 | 2.14 | -0.84 | -0.51 | -0.22 | 0.09 | 1.80 | 2.26
CdSe | M_Cd | Cu | 2.49 | 1.23 | 1.05 | -0.88 | -0.51 | -0.14 | 0.36 | 1.79 | 2.33
CdSe | M_Se | Os | 5.88 | 6.53 | 7.17 | -0.55 | -0.55 | 0.05 | 1.44 | 1.90 | 2.36
CdSe | M_i_Cd_site | F | 1.95 | 1.63 | 1.31 | -0.83 | -0.51 | -0.21 | 0.12 | 1.82 | 2.38
CdTe | M_i_Cd_site | Hg | 1.78 | 1.47 | 1.76 | -0.65 | -0.15 | 0.29 | 1.66 | 2.06 | 2.42
CdTe | M_i_old | Cu | 2.50 | 1.94 | 2.22 | -0.74 | -0.40 | 1.26 | 1.72 | 2.08 | 2.43
CdSe | M_i_Se_site | Cl | 3.68 | 3.36 | 3.03 | -0.65 | -0.32 | 0.05 | 0.38 | 1.94 | 2.51
CdTe | M_Cd | Sr | 1.06 | 1.06 | 1.06 | -0.64 | -0.41 | -0.10 | 1.66 | 2.11 | 2.52
CdS | M_i_S_site | S | 5.23 | 4.57 | 3.91 | -0.06 | -0.05 | 0.78 | 1.13 | 1.59 | 2.69
CdS | M_i_Cd_site | S | 4.81 | 4.15 | 3.49 | -0.56 | -0.27 | 0.56 | 1.02 | 1.50 | 2.71
CdS | M_Cd | O | 7.52 | 6.22 | 5.56 | -0.87 | -0.30 | 0.10 | 0.47 | 2.11 | 2.75
CdS | M_i_old | S | 4.65 | 3.99 | 3.33 | -0.65 | 0.83 | 0.83 | 1.48 | 1.95 | 2.75
CdSe | M_i_Se_site | Pd | 2.22 | 1.58 | 2.02 | -0.62 | -0.19 | 0.27 | 1.56 | 2.09 | 2.89
CdS | M_Cd | S | 6.04 | 4.73 | 3.42 | -0.80 | 0.46 | 0.83 | 1.32 | 2.32 | 2.94
CdSe | M_Cd | Pb | 0.76 | 0.73 | 0.74 | -0.68 | -0.16 | 0.34 | 1.67 | 2.19 | 2.97
CdS | M_i_old | Pt | 3.03 | 2.38 | 3.25 | -0.43 | 0.23 | 0.72 | 1.98 | 2.57 | 3.38
CdS | M_S | Se | 0.19 | 0.20 | 0.21 | -0.77 | -0.42 | -0.12 | 1.95 | 2.53 | 3.39
Dataset 1: Formation Enthalpies (∆H)  945 impurities  945 points (each)
Dataset 2: Charge Transition Levels (𝜀(q1/q2))  381 impurities  2286 points (combined)

## Slide 5
Root mean square error (RMSE) between DFT and experiments
= 0.22 eV
ML models with similar accuracy can replace DFT computations and lead to accelerated screening.
𝜀(q1/q2): DFT vs Experiments
CdTe
4
"Machine-learned impurity level prediction for Cd chalcogenides”, npj Comput. Mater. (2020).

## Slide 6
Correlation between descriptors & properties
Descriptors from unit cell defect calculations show largest correlations.
Unit cell defect VBM & CBM have > 80% correlation with +1/0 & -1/0 transition levels.
Unit cell defect ∆H is 90% correlated with supercell ∆H.
Unit cell defect calculation
Elemental properties of M
DATASET: ~ 400 impurities in CdTe, CdSe and CdS.
Impurity simulated in an 8 atom unit cell; two orders of magnitude cheaper calculation
5

## Slide 7: Descriptors for Machine Learning
CdX | Doping Site | M | Delta Ion. En. | Delta At. Rad. | Delta EN | Delta Val. | … | Unit_cell_def CBM | Unit_cell_def ∆H(Mod) | Unit_cell_def ∆H(X-rich)
CdTe | M_Te | N | -347.5 | 0.061 | -0.71 | -1 |  | 1.156 | 1.048 | 0.812
CdTe | M_Te | O | -371.9 | 0.411 | -0.76 | -1 |  | 1.316 | 1.173 | 1.083
CdTe | M_i_Te_site | Rh | -448.9 | 0.861 | -0.87 | -1 |  | 1.647 | 1.942 | 1.965
CdTe | M_Te | Re | -464.7 | 0.991 | -0.87 | 2 |  | 2.140 | 2.326 | 2.481
CdSe | M_Se | Si | -492 | 1.181 | -0.9 | -1 |  | 2.000 | 3.000 | 3.000
CdTe | M_Cd | Be | 31.7 | -0.369 | -0.12 | 0 |  | 2.718 | 0.770 | 0.651
CdTe | M_i_Cd_site | F | -130 | 0.111 | -0.38 | 0 |  | 2.907 | 0.113 | 0.114
CdTe | M_i_Te_site | F | -277.9 | 0.481 | -0.69 | 0 |  | 2.995 | 0.864 | 0.865
CdSe | M_Cd | Cu | -318.2 | 0.661 | -0.74 | 0 |  | 2.995 | 1.276 | 1.277
CdSe | M_Se | Os | -364.8 | 0.731 | -0.8 | 0 |  | 2.897 | 1.807 | 1.808
CdSe | M_i_Cd_site | F | -67.1 | -0.509 | 0.35 | 1 |  | 3.300 | 3.320 | 2.846
CdTe | M_i_Cd_site | Hg | -290.1 | -0.059 | -0.08 | 1 |  | 3.547 | 0.954 | 1.214
CdTe | M_i_old | Cu | -288.9 | -0.079 | 0.12 | 1 |  | 3.032 | 0.757 | 0.856
CdSe | M_i_Se_site | Cl | -309.4 | 0.171 | 0.09 | 1 |  | 3.327 | 0.723 | 0.920
CdTe | M_Cd | Sr | -278.4 | 0.221 | 0.35 | 1 |  | 2.854 | 0.999 | 0.796
CdS | M_i_S_site | S | 218.7 | -0.579 | 0.86 | 2 |  | 3.506 | 5.499 | 5.025
CdS | M_i_Cd_site | S | -81.3 | -0.169 | 0.21 | 2 |  | 3.408 | 1.755 | 1.281
CdS | M_Cd | O | -105.6 | -0.119 | 0.32 | 2 |  | 3.541 | 0.897 | 0.737
CdS | M_i_old | S | -159.1 | 0.131 | 0.27 | 2 |  | 3.491 | 1.076 | 1.077
CdSe | M_i_Se_site | Pd | -152.2 | 0.261 | 0.64 | 2 |  | 3.457 | 0.980 | 0.981
CdS | M_Cd | S | 534.6 | -0.569 | 1.35 | 3 |  | 2.140 | 4.523 | 3.970
CdSe | M_Cd | Pb | 144 | -0.209 | 0.5 | 3 |  | 2.945 | 2.574 | 2.045
CdS | M_i_old | Pt | 79.3 | -0.099 | 0.47 | 3 |  | 3.116 | 1.953 | 1.502
CdS | M_S | Se | -34 | 0.101 | 0.36 | 3 |  | 3.375 | 4.104 | 4.342
Descriptor Set 1: Elemental Properties (14 features)
Descriptor Set 2: Unit Cell Defect Properties (5 features)
Descriptor Set 3: Elemental + Unit Cell (19 features)
6

## Slide 8
Steps Involved in Training a Material  Property Regression Model
7
READ DATA: Labels, computed properties, descriptors.
SELECT ML TECHNIQUE: Random Forest / Kernel Ridge / LASSO / etc.
TRAIN DEFAULT MODEL: With a (for eg.) 70-30 training-test split, train a model using chosen technique.
HYPERPARAMETER OPTIMIZATION: Improve model by tuning every hyperparameter to minimize test prediction error.
CROSS-VALIDATION: Divide training data into n folds, tune hyperparameters to minimize cross-validation test error.
LEARNING CURVES: Model prediction performance vs training set size.
DEPLOY BEST MODEL: Make new predictions and discovery.

## Slide 9
Random Forest: Formation Enthalpy
Models trained for ∆H (Cd-rich) on CdTe+CdSe+CdS data
Elemental properties + unit cell defect properties lead to best models.
"Machine-learned impurity level prediction for Cd chalcogenides”, npj Comput. Mater. (2020).
8

## Slide 10
∆H (Cd-rich) (eV)
∆H (X-rich) (eV)
CdTe
CdSe
CdS
Random Forest: Formation Energy
RMSE
Training: 0.30 eV
Test: 0.40 eV
Outside: 0.55 eV
9

## Slide 11
Random Forest: Impurity Levels
Models trained for 𝜀(q1/q2) on CdTe+CdSe+CdS data
Elemental properties + unit cell defect properties lead to best models.
"Machine-learned impurity level prediction for Cd chalcogenides”, npj Comput. Mater. (2020).
10

## Slide 12
Random Forest: Transition Levels
CdTe
CdSe
CdS
Test RMSE:
0.30 eV
Outside RMSE:
0.35 eV
RF Model to predict 𝜀(q1/q2) (eV)
Out-of-sample prediction
11

## Slide 13
Impurity Formation Energies:
DFT vs ML
ML models trained on dataset of 381 impurities in CdTe, CdSe & CdS are used to predict complete formation energies for 1827 impurities in 5 compounds; in theory applicable to any impurity in any Cd-Te-Se-S compound.
12

## Slide 14: Acknowledgements
LCRC
CONTACT: mannodiarun@anl.gov
Argonne LDRD: Office of Science #DE-AC02-06CH11357
EERE PVRD: SunShot program #DOE DEEE005956.
13

## Slide 15: THANK YOU